TECHNICAL INFORMATION

PRODUCT INTENDED ONLY

FOR PROFESSIONAL USE

PROFI RS

FAST WAX

PRODUCT DESCRIPTION

PROFI RS FAST WAX is a product for all types of paints, car paints (including HS, 2K, nitro, synthetic and plastic, rubber, dashboard, gel coat, glass, mirrors, etc.). Polishing provides a perfect look and a protective coating also for various difficult coatings. Perfectly removes all traces of abrasives, mists etc. and at the same time works antistatic creating additional protection. The agent can be applied manually or mechanically using a soft sponge. It does not contain silicone and silica.

PHISICAL AND CHEMICAL PROPERTIES

- Composition:		Emulsion developed using nanotechnology, PTFE and additives

- Appearance:		liquid

- Capacity:		500 ml

- Viscosity:		9 s. (Ford cup Ø4 mm)

- Density:		1 kg/l

- Colour:		while

- pH:			neutral

- Solubility:		medium in water

USE

- Suitable for all types of high gloss surfaces.

- Can be applied to plastic (outside and inside the car), glass, gaskets without leaving marks.

- Spray on the surface, then wipe with a microfiber cloth.

STORAGE

The product works best at 15 - 25⁰C.

Storage in a closed container at a temperature of 0 - 45⁰C.

WARRANTY PERIOD

18 months from the date of production.